## Slide 1: J_elastic, J_plastic calculations

## Slide 2: J_elastic, J_plastic calculations
Term Definitions:
K = stress intensity factor is used to predict the stress state near the tip of a crack due to remote/residual stresses
Kc = critical stress intensity factor is the stress at which unstable crack propagation occurs
G = energy release rate, ie. rate at which energy is transformed as a material undergoes fracture
J = integral used to calculate the strain energy release rate per unit of fracture surface area
R-curve = quantification of the principle of increasing fracture resistance, as a function of crack length

## Slide 3: J_elastic, J_plastic calculations
Following E1820:
For basic test method using a notched 3PB test,
Where J_plastic is defined as:

## Slide 4: J_elastic, J_plastic calculations
For calculating J_elastic, we first need K:

## Slide 5: J_elastic, J_plastic calculations
P_i = force applied (N)
S = span length (m)
B = specimen thickness (m)
B_N = specimen thickness between roots of the side grooves (m) – equivalent to B for our test (E399-20a 8.2.1)
a_i = crack size (m)
W = specimen depth (m)

## Slide 6: J_elastic, J_plastic calculations
Crack size, a_i, is calculated based on the CMOD measurements shown in the formulas in E399:

## Slide 7: J_elastic, J_plastic calculations
For J_plastic, we need the following terms:
…And alpha_0 = initial crack length

## Slide 8: J_elastic, J_plastic calculations
We can then solve for the final J value:
A correction factor is applied to the final J-integral